## Slide 1: Multi-scale approach to LMO

## Slide 2
DFT: Energy barriers for diffusion and intercalation in LMO
MC: Thermodynamic study with potential energy tacken from previous Mean-Field work (work in progress).
kMC: galvanostatic and potentiostatic simulations, calculation of D(x)
Numerical simulations: construction of capacity level diagram with D(x) obtained from kMC and with experimental data
Multi-scale scheme
First principles
Atomic-Molecular level
Continuum
(German/Brazilian group)
(Argentina group)
(Argentina group)
(Both groups)
SimStack

## Slide 3: LMO cathode
https://materialsproject.org/materials/mp-25015/
Li sits in tetrahedral 8a sites of oxygen tetrahedron, whereas Mn, which resides in the 16d positions, is coordinated to oxygen in the form of octahedra
Spinel structure
Cubic crystal (space group Fd3m)
The lithium intercalation/deintercalation into/from the 8a tetrahedral sites occurs at about 4 V with the maintaining of the initial cubic spinel symmetry.

## Slide 4: Mean-Field (MF) modelling
Gavilán-Arriazu et al., ChemPhysChem 2021, 22, 1–12
8a sites

## Slide 5: Monte Carlo (MC)
Finite-size effect
Comparison MF, MC and experimental
Preliminary results

## Slide 6
Background: Galvanostatic Charging
C-rate
Particle size
Sivakkumar et al. Electrochimica Acta 55 (2010) 3330–3335
Wang, R. et al.. Nature communications, 2021, 12(1), 1-10.
Numerical simulations at continuum level

## Slide 7
Level Diagrams
(submitted for publication)
Notes: Switching the parameters, we can construct 3D plots or level diagramas for different geometries as observed on the right of the screen. The range of colors represents the maximum capacity reached.